# Description

This work shall be done accordance with sections 206 and 902 of the Michigan Department of Transportation (MDOT) 2020 Standard Specifications for Construction, except as herein provided.

The material is used for backfill and as soil mass backfill for gabion faced Mechanically Stabilized Earth (MSE) walls, for gabion gravity walls, and other locations as specified in the Contract Documents.

Backfill structures with the volume and locations as shown on plans with high quality, free draining, select granular backfill, or as directed by the Engineer.

# Materials

Provide Granular Material Class II meeting the requirements of section 902 of the MDOT 2020 Standard Specifications for Construction and the requirements contained in Table 1: Select Backfill Requirements.  Material acceptance will be based on sampling and testing by the Contractor as specified in the MDOT Material Quality Assurance Procedures Manual.  The Contractor’s testing frequency shall be 1 test per 3,000 CYD and shall supply a Test Data Certification to ensure that the material meets the physical property requirements listed in this special provision.

The backfill material shall be a natural mineral aggregate, free of organic materials.  Recycled concrete will not be permitted.

Use Backfill, Select RCOC for permanent and temporary walls.  Use only natural mineral aggregate that is free of organic materials and is substantially free of shale or other soft, poor durability particles and has a magnesium sulfate soundness loss of less than 30 percent after 4 cycles.

- Unit Weight.

- Contractor Designed Items:  Unit weight as designed by contractor

### RCOC Designed Items:  xxx-xxx pounds per cubic foot.

Table 1: Select Backfill Requirements

| Property | Test Method | Requirement |
| --- | --- | --- |
| Organic Content | AASHTO T 267 | 1.0 percent (maximum) |
| Resistivity | AASHTO T 288 | 30 ohm-m (minimum) |
| pH | AASHTO T 289 | 5-10 |
| Sulfates (a) | AASHTO T 290 | 200 ppm (maximum) |
| Chlorides (a) | AASHTO T 291 | 100 ppm (maximum) |
| Plasticity Index | AASHTO T 90 | 6 (maximum) |
| Angle of Internal Friction (b) | AASHTO T 236 (Direct Shear Test) | 34 degrees (minimum) |
| - If the resistivity is greater than or equal to 50 ohm-m, the chlorides and sulfates requirements are waived. Alternate test method ASTM 4327 (Ion Chromatography) may be used to determine sulfates and chlorides concentrations. - Use material passing the #10 sieve compacted to 95 percent of AASHTO T99, methods C or D (with oversized correction per Note 7) at optimum moisture content. No testing is required for backfills where 80 percent of sizes are greater than 0.75 inches. |  |  |

- Construction

## Backfill Placement for Gravity Walls

Backfill according to section 206, Excavation and Backfill of Structures, of the 2020 MDOT Standard Specifications for Construction and according to the Gravity Wall Special Provision.

## Backfill Placement for Mechanically Stabilized Earth (MSE) Walls

Backfill according to section 206, Excavation and Backfill of Structures, of the 2020 MDOT Standard Specifications for Construction and according to the MSE Wall Special Provision.

# Measurement and Payment

# The completed work, as described, will be measured and paid for at the contract unit price using the following pay item:

Pay Item                                                                                                    Pay Unit

Backfill, Select, RCOC…….………………………………………………..Cubic Yard

The Engineer will base payment for Backfill, Select, RCOC on plan quantity, in accordance with subsection 109.01.A. The Engineer will not measure material placed outside the maximum pay limits shown on the plans.  Payment for Backfill, Select, RCOC includes all equipment, materials, Contractor testing/certification of materials, and labor to furnish, place, and compact backfill material.

the material.